## Slide 1: 2024-07-03_S20-S21-S22-S23
Sxx_Icell_txxxx_Cxxxx_J01
Gottfrid Olsson

## Slide 2: Goals with this session
Investigate how the deposition of Li is affected by
  10 cycles of plating/stripping (S20, S21)
  Using LFP (10mm diameter) as cathode instead of Li-metal (5mm diameter)

## Slide 3: I’ll use 10kV3.0nA
SED multiplier voltage: 1530
Contrast: 26
Brightness:
  Coarse: 71
  Fine: 50

## Slide 4: S20_Icell_t1800_C0010_J01; plating/stripping with final deposition

## Slide 5: S20: top edge of sample

## Slide 6: Changed to
SED multiplier voltage: 1560
Contrast: 28
Brightness:
  Coarse: 71
  Fine: 50

## Slide 7: S20: moving down

## Slide 8: S20:

## Slide 9: S20:

## Slide 10: S20:

## Slide 11: S20:

## Slide 12: S20:

## Slide 13: S20:

## Slide 14: S20:

## Slide 15: S20:

## Slide 16: S20:

## Slide 17: S20:

## Slide 18: S20:

## Slide 19: S20: left edge of sample

## Slide 20: S20: moving right in steps of dx=0.75mm

## Slide 21: S20:

## Slide 22: S20:

## Slide 23: S20:

## Slide 24: S20:

## Slide 25: S20:

## Slide 26: S20:

## Slide 27: S20:

## Slide 28: S20:

## Slide 29: S20:

## Slide 30: S20:

## Slide 31: S20:

## Slide 32: S20:

## Slide 33: S20: learning points
See deposited Li
But, there is a large variation in sized and shapes
  Some very small Li parts, some very large structures
  No clear 5 mm Li disk of deposition, looks like Li over a much larger area on the Cu
This measurement would Not be suitable for image analysis

## Slide 34: (next sample)

## Slide 35: S21_Icell_t1800_C0000_J01; plating and stripping, last cycle was stripping

## Slide 36: S21: top edge, moving down, dy=0.75mm

## Slide 37: S21:

## Slide 38: S21:

## Slide 39: S21: north-west edge of deposition?

## Slide 40: S21:

## Slide 41: S21:

## Slide 42: S21:

## Slide 43: S21:

## Slide 44: S21:

## Slide 45: S21:

## Slide 46: S21:

## Slide 47: S21:

## Slide 48: S21: (another sample lays on top of this one)

## Slide 49: S21: left edge of sample, moving right dx=0.75mm

## Slide 50: S21:

## Slide 51: S21:

## Slide 52: S21:

## Slide 53: S21:

## Slide 54: S21:

## Slide 55: S21:

## Slide 56: S21:

## Slide 57: S21:

## Slide 58: S21:

## Slide 59: S21:

## Slide 60: S21:

## Slide 61: S21:

## Slide 62: S21:

## Slide 63: S21: learning points
See Li deposited, despite having stripped the same amount as was deposited in each cycle (and ended after the last stripping of Li)
Inhomogenous Li
Some very small Li that looks like Li that has been stripped (see article Josef sent by mail), but also larger Li structures

## Slide 64: (next sample)

## Slide 65: S22_Icell_t0000_C0050_J01; LFP/Cu, deposition directly without passivation

## Slide 66: S22: top edge of sample, moving down dy=1.0mm

## Slide 67: S22:

## Slide 68: S22:

## Slide 69: S22: larger scratch-marks here is likely due to me accidentally scratching the surface with the pincer during washing or handling of the Cu after cycling

## Slide 70: S22:

## Slide 71: S22:

## Slide 72: S22:

## Slide 73: S22:

## Slide 74: S22:

## Slide 75: S22:

## Slide 76: S22:

## Slide 77: S22:

## Slide 78: S22: left edge, moving right dx=1.0mm

## Slide 79: S22:

## Slide 80: S22:

## Slide 81: S22:

## Slide 82: S22:

## Slide 83: S22:

## Slide 84: S22:

## Slide 85: S22:

## Slide 86: S22:

## Slide 87: S22:

## Slide 88: S22: (kom utanfor kanten vid denna bild)

## Slide 89: S22: learning points
Small black ‘holes’(?) observed in the Cu
Li deposition clearly uneven despite using LFP as cathode material
  Uneven Li ‘globally’ and ‘locally’
  Some larger structures observed

## Slide 90: (next sample)

## Slide 91: S24_Icell_t000_C0050_J01; LFP deposited without passivation

## Slide 92: S24: top edge of sample, moving down, dy=1.0mm

## Slide 93: S24:

## Slide 94: S24:

## Slide 95: S24:

## Slide 96: S24:

## Slide 97: S24:

## Slide 98: S24:

## Slide 99: S24:

## Slide 100: S24:

## Slide 101: S24:

## Slide 102: S24:

## Slide 103: S24: left edge, moving right dx=1.0mm

## Slide 104: S24:

## Slide 105: S24:

## Slide 106: S24:

## Slide 107: S24:

## Slide 108: S24:

## Slide 109: S24:

## Slide 110: S24:

## Slide 111: S24:

## Slide 112: S24:

## Slide 113: S24: right edge

## Slide 114: S24: learning points
Much more even deposition (the unevenness is more or less the same ‘everywhere’, at least in more places than S23)
Small black spots (‘holes?’) observed for this sample too (LFP used in both)