## Slide 1: 2024-06-19_S06-S07-S08-S09
Sxx_Icell_t1800_Cxxxx_J01
Gottfrid Olsson

## Slide 2: Goals with this session
Investigate what values of deposited capacity of Li can be measured in the SEM for the I-cell (for good passivation, t=1800s)
How even the deposition is in the I-cell
Test the suggested data acquisition scheme (e.g. 9 or 16 images evenly spaced in the circle of deposited Li)

## Slide 3: I’ll try 10kV3.0nA

## Slide 4: S06_Icell_t1800_C0001_J01; (1 muAh/cm2)

## Slide 5: S06_M1 (matrix-position 1 of 9)

## Slide 6: S06_ due to lack of Li, take only M1, M5, M9 (but the program crashed before taking M9)

## Slide 7: S06_M5; bubbles when zooming in…

## Slide 8: S06 close to middle; hard to claim that there is Li here

## Slide 9: S06; closer to edge, maybe Li, maybe not

## Slide 10: S06: learning points
Hard to say if we can see C0001 from this measurement

## Slide 11: S07_Icell_t1800_C0003_J01; (3 muAh/cm2)

## Slide 12: S07: top edge

## Slide 13: S07; below; bubbled when zoom-in…

## Slide 14: S07; further down; again bubbles when zoom-in…

## Slide 15: S07; further down; no bubbles

## Slide 16: S07; below

## Slide 17: S07; Li? Or smth else…

## Slide 18: S07; another place; white=Li?, dark spots

## Slide 19: S07

## Slide 20: S07

## Slide 21: S07: same place as before; worms/needles?

## Slide 22: S07: same place, high mag.: close by, high mag.

## Slide 23: S07; further down

## Slide 24: S07: another place

## Slide 25: S07: learning points
Clear Li deposition at some points, even for this sample’s C0003
  But only at certain regions, not true for the whole Li deposition area
However, not all Li is nice crystalline particles
  Saw worms or needles (very small/short); as we saw in sample Y (master’s thesis)

## Slide 26: S08_Icell_t1800_C0010_J01; (10 muAh/cm2)

## Slide 27: S08; at edge

## Slide 28: S08: down; edge of deposition

## Slide 29: S08: down further; Li

## Slide 30: S08; same place as before; halos around Li?

## Slide 31: S08; same place; small Li nuclei

## Slide 32: S08; further down; inhomogenous Li deposition

## Slide 33: S08; further down; inhomogenous Li deposition

## Slide 34: S08; slightly right of the place before

## Slide 35: S08: another place; inhomogenous Li dep.

## Slide 36: S08; another place, inhomogenous Li

## Slide 37: S08: another place

## Slide 38: S08: another place

## Slide 39: S08: images for AI-training or analysis

## Slide 40: S08: images for AI-training or analysis: reasonable magnification for C0010: 3k to 7k?

## Slide 41: S08: images for AI-training or analysis: reasonable magnification for C0010: 4k to 6k?

## Slide 42: S08: images for AI-training or analysis

## Slide 43: S08: images for AI-training or analysis (several images at 6k mag.)

## Slide 44: S08: images for AI-training or analysis (several images at 6k mag.)

## Slide 45: S08: images for AI-training or analysis (several images at 6k mag.)

## Slide 46: S08: images for AI-training or analysis (several images at 5k mag.)

## Slide 47: S08: images for AI-training or analysis (several images at 5k mag.)

## Slide 48: S08: images for AI-training or analysis (several images at 5k mag.)

## Slide 49: S08: previous 5k/6k mag images taken in this region

## Slide 50: S08: learning points
Clear Li deposition with nice crystalline particles for C0010
However, still inhomogeneous (but significantly more even than the C-cell)
Li particles have white ‘halos’ around them
Around 5k magnification might be suitable for image analysis

## Slide 51: S09_Icell_t1800_C0030_J01; (30 muAh/cm2)

## Slide 52: S09: top edge

## Slide 53: S09; down

## Slide 54: S09; down

## Slide 55: S09; down, large dark region (bad clean probably, but how?) was dark all the way down

## Slide 56: S09; left edge

## Slide 57: S09; moving right; looks like some dirt/dark stuff too

## Slide 58: S09; Li;

## Slide 59: S09

## Slide 60: S09; needle-growth, ‘large’ and small

## Slide 61: S09: same place, Josef: might be salt. Right: more stuff that’s joined together!

## Slide 62: S09: close by, large area of worms/small needles

## Slide 63: S09; further right

## Slide 64: S09;

## Slide 65: S09; further right

## Slide 66: S09; same place, more zoom (left) and then at a later time (right)

## Slide 67: S09; right, bubbles when zoom

## Slide 68: S09
Deposited Li for C0030
  Worms/needles as we saw before - but this time very much worms and only some areas of nice particles
Bad washing in some places

## Slide 69: Acquisition scheme & EP
Very hard to say where the Li deposition starts and not
  Maybe manually pick a ‘center’ point and take the matrix square pictures w.r.t that center
Electropolishing seems to have made the Cu surface more smooth (almost no grinding-marks left)