## Slide 1: 2024-06-25_S12-S13-S14-S15
Sxx_Icell_txxxx_Cxxxx_J01
Gottfrid Olsson

## Slide 2: Goals with this session
Investigate the same conditions for samples S07, S09 which had unusual deposition and/or bad washing (S14, S15)
Investigate same C0010 for different passivation (S12, S13)
Test data acquisition scheme (3x3 square matrix based on center point chosen manually)

## Slide 3: I’ll use 10kV3.0nA

## Slide 4: S12_Icell_t0012_C0010_J01

## Slide 5: S12: top edge

## Slide 6: S12:moving down

## Slide 7: S12: looks like bad washing, but no bubbles

## Slide 8: S12: down, looks cleaner here

## Slide 9: S12: top edge of deposition

## Slide 10: S12: top edge of deposition

## Slide 11: S12

## Slide 12: S12: choosing X5000 magnification for the images image analysis

## Slide 13: S12 further down; worms at this part

## Slide 14: S12: matrix squares with dx=dy=500mu

## Slide 15: S12: M1

## Slide 16: S12: M2

## Slide 17: S12: M3

## Slide 18: S12: M4

## Slide 19: S12: M5 (matrix square 5 image of 9)

## Slide 20: S12: M6

## Slide 21: S12: M7

## Slide 22: S12: M8

## Slide 23: S12: M9

## Slide 24: S12: different deposition in different areas

## Slide 25: S12: same area; worm-like structures with barren areas in between

## Slide 26: S12: same area; worm-like structures with barren areas in between && Li nuclei particles

## Slide 27: S12: another area further away; Li particles

## Slide 28: S12: another area, Li nuclei

## Slide 29: S12: learning points
Li is unevenly deposited: clearly more in some places than others (locally too)
Saw areas with worm-like structures
  with barren areas between areas of worm-like structures, but also Li nuclei mixed in
Saw areas with only Li nuclei

## Slide 30: S13_Icell_t0060_C0010_J01

## Slide 31: S13

## Slide 32: S13; edge of sample, moving downwards

## Slide 33: S13: edge of deposition

## Slide 34: S13; just below the top edge of deposition

## Slide 35: S13: further down (less deposition than in the edge of the deposition)

## Slide 36: S13: further down, more Li again

## Slide 37: S13: further down, big ‘hole’
Suuuper small Li?

## Slide 38: S13;

## Slide 39: S13; edge of ‘hole’

## Slide 40: S13; below, particles of various size

## Slide 41: S13; moving down – much more evenly deposited here compared to S12

## Slide 42: S13; end of Li(?), why wavy and sudden edge? Also much smaller compare to last slide

## Slide 43: S13; looks like smth was on the surface, edge of ring of that smth

## Slide 44: S13; moving up along left EoD; super small Li

## Slide 45: S13: zoom in on some black dirt?

## Slide 46: S13

## Slide 47: S13; the very small Li – corroded Li? They are much smaller and have weird shapes

## Slide 48: S13; another place, dark Li?

## Slide 49: S13; needle-like structures observed already at C0010

## Slide 50: S13; matrix sampling dx=dy=1 mm

## Slide 51: S13; M1

## Slide 52: S13; M2

## Slide 53: S13; M3

## Slide 54: S13; M4

## Slide 55: S13; M5

## Slide 56: S13; M6

## Slide 57: S13; M7

## Slide 58: S13; M8

## Slide 59: S13; M9

## Slide 60: S13: learning points
Still a bit uneven Li deposition, but MUCH more even compared to S12
  Should be good enough to do matrix-sampling and image analysis on
Various sizes of Li nuclei at the same time (position/SEM image)
Matrix-sampling seems to be a good idea
  Easy and quite fast
  Perhaps allow some finer manual adjustment of position (e.g. do not take in a ‘hole’ but rather the closest area to that ‘hole’ where there is Li instead)

## Slide 61: S14_Icell_t1800_C0003_J01

## Slide 62: S14: top edge

## Slide 63: S14 : top EoD

## Slide 64: S14; dark Li, some worm-like shapes also

## Slide 65: S14; moving down, lots of no Li. Zooming in on one big bright thing – it moves when imaged

## Slide 66: S14; bad wash again? :(

## Slide 67: S14; another place

## Slide 68: S14: following the deposition ring upwards

## Slide 69: S14; many larger pieces of dirt on this sample

## Slide 70: S14: left EoD, moving inwards 

## Slide 71: S14;

## Slide 72: S14; more right

## Slide 73: S14;

## Slide 74: S14; more right

## Slide 75: S14; learning points
Looks like there is a ring-like deposition area (like in the coin cell)
  more Li for large radii and less for smaller radii (measured from the center of the Li deposition)
No worm-like structures observed

## Slide 76: S15; a lot of shite (bad wash >:( …)

## Slide 77: S15: close to edge (right); stripey

## Slide 78: S15; following the ‘valley’ towards the middle

## Slide 79: S15; looking at the dirt/shite (further down)

## Slide 80: S15; mostly bad washing, some parts have clear Li particles, e.g.

## Slide 81: S15: learning points
Bad wash (a LOT of large dark areas that bubbled when imaged)
  Uneven wash: totally good in a few places, very bad in most places