## Slide 1: 2024-06-27_S16-S17-S18-S19
S1x_Icell_t1800_C0010_J01
Gottfrid Olsson

## Slide 2: Goals with this session
Reproducibility after changes to method: are the properties of the samples the same? If they differ, how?
SEM images in a 4x4 grid for image analysis
  Test of 4x4 sampling
  Images for training (images taken close to the grid-images)
  Images for analysis (4x4 grid)

## Slide 3: I’ll use 10kV3.0nA
Nice imaging achieved:

## Slide 4: S16_Icell_t1800_C0010_J01
Cu polished to P4000 then electropolished

## Slide 5: S16: top edge

## Slide 6: Testing different SED multiplier V and contrast, brightness

## Slide 7: Testing different SED multiplier V and contrast, brightness
For now, 10kV, 3nA
SED multiplier voltage 1560
Contrast 30 %, brightness 71% coarse, 45% fine

## Slide 8: S16: moving down; edge of deposition
Notes: Clear halo around Li nuclei; flackig Cu yta, pga elektropolering?

## Slide 9: S16: down, uneven deposition

## Slide 10: S16: down, right: pretty even deposition

## Slide 11: S16: down

## Slide 12: S16: down, less even deposition; also streaks of Li: left picture is further down

## Slide 13: S16: down; left: up and left – bubbles, locally bad wash

## Slide 14: S16: up, left

## Slide 15: S16: grid SEM images squares, dx=dy=750mu

## Slide 16: Position 1 of 16 (I’ll take zoomed out pics too, until we know that the deposition is even)
Notes: Löpande nummer: 1

## Slide 17: Position 2 of 16
Notes: Löpande nummer: 2

## Slide 18: Position 3 of 16
Notes: Löpande nummer: 3

## Slide 19: Position 4 of 16
Notes: Löpande nummer: 4

## Slide 20: Position 8 of 16
Notes: Löpande nummer: 5

## Slide 21: Position 7 of 16
Notes: Löpande nummer: 6

## Slide 22: Position 6 of 16
Notes: Löpande nummer: 7

## Slide 23: Position 5 of 16
Notes: Löpande nummer: 8

## Slide 24: Position 9 of 16
Notes: Löpande nummer: 9

## Slide 25: Position 10 of 16
Notes: Löpande nummer: 10

## Slide 26: Position 11 of 16
Notes: Löpande nummer: 11

## Slide 27: Position 12 of 16
Notes: Löpande nummer: 12

## Slide 28: Position 16 of 16
Notes: Löpande nummer: 13

## Slide 29: Position 15 of 16
Notes: Löpande nummer: 14

## Slide 30: Position 14 of 16
Notes: Löpande nummer: 15

## Slide 31: Position 13 of 16
Notes: Löpande nummer: 16 (slut); shiet, bubblade vid zoom-in

## Slide 32: S16: some AI training images, taken at spots with clear Li/Cu separation (around point 8)
Notes: Löpande nummer: 16 (slut)

## Slide 33: S16: learning points
Li deposition pretty okay evenly distributed
  Although some parts barren of Li
Washing is still weird with some parts covered in shite, but most of this sample looked good
4x4 grid sampling seems even better than 3x3 and won’t take that long if only the zoomed-in image is taken
  The long time waste is waiting for the SmartSoft program

## Slide 34: (next sample)

## Slide 35: S17_Icell_t1800_C0010_J01
Cu polished to P4000 then to 0.25 microns diamond slurry

## Slide 36: S17: top edge, grinding marks visible
Notes: Clear difference between EP samples and not EP (only mechanical polishing)

## Slide 37: S17: down, Li stripes (why?)

## Slide 38: S17: down; left; down, right (still stripes)

## Slide 39: S17: down

## Slide 40: S17: grid SEM images squares, dx=dy=1000mu
This sample won’t give good analysis since the Li is so uneven
Taking 3x3 pictures zoomed out for reference of uneveness

## Slide 41: Position 5 of 9
Notes: Löpande nummer: 1

## Slide 42: Position 6 of 9

## Slide 43: Position 3 of 9

## Slide 44: Position 2 of 9

## Slide 45: Position 1 of 9

## Slide 46: Position 4 of 9

## Slide 47: Position 7 of 9

## Slide 48: Position 8 of 9

## Slide 49: Position 9 of 9

## Slide 50: S17: learning points
Only mechanical polishing, even to 0.25 microns diamond slurry, results in clearly visible ‘grinding lines’. If electropolishing is done, these lines are no longer observed
This sample shows very uneven Li, with Li being observed in stripes

## Slide 51: (next sample)

## Slide 52: S18_Icell_t1800_C0010_J01
Cu polished to P4000 then to 0.25 microns diamond slurry

## Slide 53: S18: top edge

## Slide 54: S18: top edge, again grinding lines

## Slide 55: S18: sane thing, but this looks maybe like the tweezer caused this (larger mark in Cu)

## Slide 56: S18: right of previous image

## Slide 57: S18:

## Slide 58: S18:

## Slide 59: Sxx: grid SEM images squares, dx=dy=750mu

## Slide 60: Position 1 of 16
Notes: Löpande nummer: 1

## Slide 61: Position 2 of 16
Notes: Löpande nummer: 2

## Slide 62: Position 3 of 16
Notes: Löpande nummer: 3

## Slide 63: Position 4 of 16
Notes: Löpande nummer: 4

## Slide 64: Position 8 of 16
Notes: Löpande nummer: 5

## Slide 65: Position 7 of 16
Notes: Löpande nummer: 6

## Slide 66: Position 6 of 16
Notes: Löpande nummer: 7

## Slide 67: Position 5 of 16
Notes: Löpande nummer: 8

## Slide 68: Position 5 of 16
Changed:
SED multiplier voltage 1560 (unchanged)
Contrast 28 % (changed)
Brightness coarse 71 % (unchanged)
Brightness fine 30 % (changed)
Notes: Löpande nummer: 8

## Slide 69: Position 9 of 16
Notes: Löpande nummer: 9

## Slide 70: Position 10 of 16
Notes: Löpande nummer: 10

## Slide 71: Position 11 of 16
Notes: Löpande nummer: 11

## Slide 72: Position 12 of 16
Notes: Löpande nummer: 12

## Slide 73: Position 16 of 16
Notes: Löpande nummer: 13

## Slide 74: Position 15 of 16
Notes: Löpande nummer: 14

## Slide 75: Position 14 of 16
Notes: Löpande nummer: 15

## Slide 76: Position 13 of 16
Notes: Löpande nummer: 16 (slut)

## Slide 77: S18: a few AI training images (grinding lines)

## Slide 78: S18: learning points
This sample had much more even Li deposition!
Some very small Li(?) can be observed around Li particles

## Slide 79: (next sample)

## Slide 80: S19_Icell_t1800_C0010_J01

## Slide 81: S19: top edge

## Slide 82: S19: top edge of deposition; left: just below top edge of deposition

## Slide 83: S19: down, little to no Li at center of Li-disk

## Slide 84: S19: down; dark part on left-hand side…

## Slide 85: S19: a little bit down; black spots on Cu

## Slide 86: S19: uneven

## Slide 87: S19: grid SEM images squares, dx=dy=1500mu

## Slide 88: Position 5 of 9
Notes: Löpande nummer: 1

## Slide 89: Position 6 of 9

## Slide 90: Position 3 of 9

## Slide 91: Position 2 of 9

## Slide 92: Position 1 of 9

## Slide 93: Position 4 of 9

## Slide 94: Position 7 of 9

## Slide 95: Position 8 of 9

## Slide 96: Position 9 of 9

## Slide 97: S19: learning points
For some reason, very uneven deposition: looks like less than the other samples (but should be the same C0010)

## Slide 98: Summary SEM session
One really good sample, with even Li over a large area
4x4 grid sampling works too
  What dx=dy is best?
But: large differences in even/uneven Li and washing between samples
  BAD reproducibility…
  But better (more similar) wash between samples compared to previous times
No ‘worms’ observed